CYPRUS UNIVERSITY OF TECHNOLOGY

DEPARTMENT OF ELECTRICAL ENGINEERING AND

COMPUTER ENGINEERING AND INFORMATION

Move2Treat

WP3: Monolithic sensing elements using direct FSL inscription

# Study of polymer planar samples

Date:09/07/2024

Lab: Photonics and Optical Sensors Research Laboratory (PhOSLab)

# PURPOSE

Multiplexed sensors can be “squeezed” into a miniaturized sensing head, adding advanced functionality, obviating the need for complex interrogation methods, and offering high signal quality in a potentially “noisy” measurement environment. A key sensor component is the fiber Bragg grating (FBG), a wavelength-encoded, in-fiber mirror with tailored bandwidth and reflectivity. FBGs are laser inscribed into fibers, typically using ultra-violet lasers (UVL) and phase masks to create the parallel reflecting index planes in the fiber core. However, the mask’s length and period limit the grating bandwidth and operating wavelength, respectively. Also, UVL Bragg gratings in multimode optical fiber display multiple peak spectra, with overlapping Bragg modes that exchange power due to spatial mode mixing in the fiber core when perturbed by external fields; peak tracking algorithms can no longer know which peak to track. This is acceptable if low-resolution measurements can be tolerated, but not for Move2Treat. The UVL penetration depth in polymer fibers is loss limited affecting repeatability, mode excitation and Bragg grating spectral quality. FSLs have opened new territory for gratings and micro-structured fiber devices. CUT’s main foci and competencies are in optimized photonic component and sensor development using FSL inscription, for applications in sensing and fiber lasers.

Development of in-fiber sensors using FSL inscription includes fiber gratings with periodic, aperiodic and apodiing structures. CUT’s FSL plane-by-plane inscription method that produces strong (κL>5) Bragg gratings and pm-level wavelength shifts with random polarization, but importantly it is possible to produce single-peak gratings, even in multimode fibers. We will enhance the inscription accuracy using image processing. These key competencies are critical to Move2Treat, where a multi-faceted experience is required to seamlessly integrate the temperature sensors into the multifunctional fiber, without disrupting the implant’s waveguiding or operational properties. Multiple wavelength FSL inscription in the polymer fiber will be explored as this is material dependent, and FSL patterning of the fiber tip will offer careful light distribution control for appropriate tissue activation, completely integrating all components within the fibers. CUT offers FSL inscription expertise of single peak FBGs (unique in Europe and beyond) to develop ultra-sensitive miniaturized sensing elements at the tip of the optoelectronic fiber.

# EXPERIMENTAL SET-UP

The inscription setup employed for the plane-by-plane (Pl-by-Pl) inscription method consists of a femtosecond laser system (HighQ Laser femtoREGEN) operating at 517 nm with a 220-fs pulse duration and an air-bearing translation stage system (Aerotech) for accurate two-axis motion. The laser beam was guided through a series of mirrors through a long working distance microscope objective and a third translation stage controlled the focal length. Lower loss is provided as well by the choice to operate the laser in the visible (517nm) and a repetition rate of 100KHz. The inscription process was observed in real time with the use of a CCD camera. The laser pulse energy was controlled by an attenuator so it could have values from a few of nJ to μJ per pulse. The channels were inscribed by a 2-axis controlled, automated stage motion, synchronized using G-code programming allowing the implementation of complex motions (tilt, arcs, etc.). In Fig. 2 is depicted a picture of the inscription setup. The red line indicates the direction the beam of light follows directed through optics and finally through the microscope objective.

Fig. 2.1 Inscription setup for Pl-by-Pl femtosecond laser inscription method.

# CHARACTARIZATION OF POLYMER PLANAR SAMPLES